Supplementary Information

Pressure-Dependent Electronic, Optical, and Mechanical Properties of Antiperovskite X3NP (X = Ca, Mg): A First-Principles Study

Chunbao Feng1,2, Changhe Wu1, Xin Luo1, Tao Hu1, Fanchuan Chen1, Shichang Li1,2, Shengnan Duan1,2, Wenjie Hou3, Dengfeng Li1,2, †, Gang Tang4, †, and Gang Zhang5, †

1School of Science, Chongqing University of Posts and Telecommunications, Chongqing 400065, China

2Institute for Advanced Sciences, Chongqing University of Posts and Telecommunications, Chongqing 400065, China

3School of Computer Science and Technology, Northwestern Polytechnical University, Xi’an710129, China

4Advanced Research Institute of Multidisciplinary Science, Beijing Institute of Technology, Beijing 100081, China

5Institute of High Performance Computing, A*STAR, 138632, Singapore

†Corresponding Authors:

lidf@cqupt.edu.cn (D. Li), gtang@bit.edu.cn (G. Tang) and zhangg@ihpc.a-star.edu.sg (G. Zhang).

I. Computational methods

Our calculations are performed using the projector augmented wave (PAW) method implemented in the Vienna ab initio simulation package (VASP) code[1, 2]. The standard PAW pseudo potentials are adopted[3]. We use the Perdew, Burke, and Ernzerhof (PBE) form of the generalized gradient approximation (GGA) exchange correlation functional[4] for crystal structure relaxation, and the hybrid density functional (Heyd-Scuseria-Ernzerhof, HSE06)[5] for electronic properties of X3NP (X2+ = Ca, Mg). The cut-off energy of 400 eV and the k-point meshes with a grid spacing of 2π×0.02 Å-1 were used for structural relaxation. The cut-off energy and KSPACING test of X3NP (X2+ = Ca, Mg) are shown in Fig S1 and S2. After each pressure change, full volume relaxation has been done. For band structure and density of states (DOSs) calculations, the cut-off energy is set to 400 eV. In all calculations, the total energy is converged to less than 10-6 eV. During the structure optimization, the maximum force is less than 0.02 eV/Å, where the lattice constants and atomic positions are fully relaxed. The spin-orbit coupling (SOC) effect is not considered in the calculation of the electronic properties of X3NP (X2+ = Ca, Mg) because it does not significantly affect their band edges (as can be seen in Fig S4). The phonon dispersion calculations are based on PHONOPY code with a 2×2×2 supercell[6]. The electronic and optical properties were post-processed using the VASPKIT program[7]. Tight convergence criteria were adapted for the calculations of Young’s modulus and dielectric constant, for example, the cut-off energy of 700 eV for Young’s modulus calculations and the cut-off energy of 500 eV for dielectric constant calculations. The dielectric properties of the studied compounds are calculated by density functional perturbation theory (DFPT)[8]. The static dielectric constant (εstd) consists of the electronic (ɛꝏ) and the ionic parts (εion). Based on the calculated elastic constants, the ElATools program[9] is employed to obtain the orientational-dependent Young’ s modulus. Based on the method proposed by Yu, et al[10], a python code (SL3ME)[11] is used to calculate the spectroscopic limited maximum efficiency (SLME).

Fig. S1. (Color online) The cut-off energy test of (a) Ca3NP and (b) Mg3NP.

Fig. S2. (Color online) The KSPACING test of (a) Ca3NP and (b) Mg3NP.

II. Structural parameters, stability, optoelectronic properties

Table S1. Lattice parameters for Ca3NP and Mg3NP with Pnma (3D) symmetry under different pressure.

| Compounds | Pressure (GPa) | a (Å) | b (Å) | c (Å) | α = β = γ (°) | Volume (Å3) |
| --- | --- | --- | --- | --- | --- | --- |
| Ca3NP | 0 | 6.726 6.658a 6.554b | 9.424 9.452a 9.335b | 6.621 6.709a 6.655b | 90 | 419.678 |
|  | 5 | 6.584 | 9.248 | 6.491 | 90 | 395.229 |
|  | 10 | 6.432 | 9.100 | 6.385 | 90 | 373.722 |
|  | 15 | 6.321 | 8.978 | 6.294 | 90 | 357.184 |
|  | 20 | 6.223 | 8.868 | 6.214 | 90 | 342.923 |
| Mg3NP | 0 | 5.900 5.887b | 8.337 8.309b | 5.911 5.875b | 90 | 290.752 |
|  | 5 | 5.814 | 8.233 | 5.835 | 90 | 279.302 |
|  | 10 | 5.728 | 8.127 | 5.754 | 90 | 267.857 |
|  | 15 | 5.655 | 8.038 | 5.683 | 90 | 258.320 |
|  | 20 | 5.592 | 7.961 | 5.620 | 90 | 250.191 |

aRef.,12 bRef.13

From Table S1, it can be seen that the total energy differences between X3NP (X= Ca, Mg) (space group Pnma) one-dimension (1D) and three-dimension (3D) are given in Table S2, which shows that Ca3NP maintains the Pnma phase from 0 to 20 GPa, meanwhile there is no phase transition in Mg3NP from 0 to 20 GPa range. The phonon spectra of X3NP (X = Ca, Mg) for the orthorhombic phase with Pnma space group (SG) are also illustrated in Fig. S3 which indicate that they are dynamic stability from 5 to 20 GPa.

Table S2. The total enthalpy (H = E+PV) difference of Ca3NP and Mg3NP between Pnma (1D) and Pnma (3D) space group (SG) under different pressure.

| Pressure (GPa) | Ca3NP |  |  | Mg3NP |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Pnma (1D) (eV/f.u.) | Pnma (3D) (eV/f.u.) | ΔH=Htot(1D)-Htot(3D) (eV/f.u.) | Pnma (1D) (eV/f.u.) | Pnma (3D) (eV/f.u.) | ΔH=Htot(1D)-Htot(3D) (eV/f.u.) |
| 0 | -96.569 | -99.225 | 2.656 | -21.309 | -22.071 | 0.762 |
| 5 | -85.268 | -86.432 | 1.164 | -19.002 | -19.776 | 0.774 |
| 10 | -73.531 | -74.449 | 0.918 | -16.865 | -17.643 | 0.778 |
| 15 | -62.474 | -63.054 | 0.580 | -14.816 | -15.592 | 0.776 |
| 20 | -52.126 | -52.134 | 0.009 | -12.840 | -13.609 | 0.769 |
| 25 | -42.011 | -41.613 | -0.397 | -10.927 | -11.685 | 0.759 |
| 30 | -32.244 | -31.434 | -0.810 | -9.067 | -9.813 | 0.746 |
| 35 | -22.780 | -21.555 | -1.226 | -7.255 | -7.987 | 0.731 |
| 40 | -13.590 | -11.942 | -1.648 | -5.487 | -6.202 | 0.715 |

Fig. S3. (Color online) Phonon Spectra of Ca3NP and Mg3NP with Pnma (3D) symmetry under different pressure. (a) 5 GPa, (b) 10 GPa, (c) 15 GPa, and (d) 20 GPa for Ca3NP. (e) 5 GPa, (f) 10 GPa, (g) 15 GPa, and (h) 20 GPa for Mg3NP.

Fig. S4. (Color online) Band structures of Ca3NP from (a) HSE and (b) HSE+SOC method at 0 GPa. Note that SOC has a negligible effect on the band-edge dispersion. Therefore, only HSE06 method was employed in our calculations.

Fig. S5. (Color online) Band structures and PDOS of Ca3NP under different pressure from HSE06 method. (a), (c) 0 GPa and (b), (d) 20 GPa. (b) and (d) is aligned with a and c using the Cs 5s core level energy respectively.

Fig. S6. (Color online) Band structures and PDOS of Mg3NP under different pressure from HSE06 method. (a), (c) 0 GPa and (b), (d) 20 GPa. (b) and (d) is aligned with a and c using the Cs 5s core level energy respectively.

Fig. S7. (Color online) Band structures of Ca3NP and Mg3NP with Pnma (3D) symmetry under different pressure. (a) 0 GPa, (b) 5 GPa, (c) 10 GPa, and (d) 15 GPa for Ca3NP. (e) 0 GPa, (f) 5 GPa, (g) 15 GPa, and (h) 15 GPa for Mg3NP. The black, red, green dot mean cation atom, P atom and N atom donation respectively. The band structures under different pressure are aligned with the band structure at 0 GPa using the Cs 5s core level energy. The dash line refers for CBM (red) and VBM (blue) of X3NP (X = Ca, Mg) at 0 GPa. It is not the Fermi energy level.

Table S3. The hole and electron effective masses of Ca3NP and Mg3NP under different pressure.

| Compounds | Pressure (GPa) | hole |  |  | electron |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Γ-X | Γ-Y | Γ-Z | Γ-X | Γ-Y | Γ-Z |
| Ca3NP | 0 | 0.226 | 0.817 | 0.864 | 0.550 | 0.333 | 0.708 |
|  | 5 | 0.244 | 0.721 | 0.742 | 0.553 | 0.304 | 0.727 |
|  | 10 | 0.231 | 0.638 | 0.604 | 0.553 | 0.277 | 0.710 |
|  | 15 | 0.246 | 0.520 | 0.532 | 0.548 | 0.265 | 0.694 |
|  | 20 | 0.229 | 0.521 | 0.483 | 0.539 | 0.259 | 0.674 |
| Mg3NP | 0 | 0.145 | 0.988 | 0.570 | 0.204 | 0.567 | 0.238 |
|  | 5 | 0.159 | 0.681 | 0.604 | 0.204 | 0.610 | 0.223 |
|  | 10 | 0.157 | 0.842 | 0.510 | 0.202 | 0.622 | 0.212 |
|  | 15 | 0.163 | 0.858 | 0.468 | 0.199 | 0.621 | 0.205 |
|  | 20 | 0.164 | 0.938 | 0.430 | 0.196 | 0.619 | 0.199 |

Table S4. Band gap Eg (eV), electronic dielectric constant εꝏ, ionic dielectric constant εion, Young's module Y (GPa), average electron effective mass me (m0), average hole effective mass mh (m0), valence band width Wvb(eV), exciton binding energy Eb (eV) of Ca3NP and Mg3NP under different pressure.

| Compounds | Pressure (GPa) | Eg (eV) | εꝏ | εion | Y (GPa) | me (m0) | mh (m0) | Wvb (eV) | Eb (meV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca3NP | 0 | 2.136 | 7.533 | 15.800 | 104.935 | 0.530 | 0.636 | 3.000 | 69 |
|  | 5 | 2.083 | 7.500 | 12.967 | 116.224 | 0.528 | 0.569 | 3.128 | 66 |
|  | 10 | 1.956 | 7.600 | 11.867 | 128.126 | 0.513 | 0.491 | 3.302 | 60 |
|  | 15 | 1.857 | 7.667 | 11.167 | 136.034 | 0.502 | 0.433 | 3.432 | 54 |
|  | 20 | 1.767 | 7.767 | 10.667 | 141.747 | 0.491 | 0.411 | 3.554 | 50 |
| Mg3NP | 0 | 2.366 | 8.767 | 18.300 | 166.630 | 0.336 | 0.568 | 5.722 | 37 |
|  | 5 | 2.364 | 8.600 | 16.033 | 181.311 | 0.346 | 0.481 | 5.928 | 37 |
|  | 10 | 2.349 | 8.500 | 14.067 | 193.838 | 0.345 | 0.503 | 6.144 | 38 |
|  | 15 | 2.327 | 8.467 | 12.633 | 201.059 | 0.342 | 0.496 | 6.331 | 38 |
|  | 20 | 2.300 | 8.400 | 11.600 | 203.470 | 0.338 | 0.511 | 6.499 | 39 |

Fig. S8. (Color online) The optical absorption of (a) Ca3NP and (b) Mg3NP under 0 GPa (line) and 20 GPa (dot). The black, red and blue means xx, yy and zz direction donation, respectively.

III. Mechanical and dielectric properties

For an orthorhombic structure (SG Pnma), the conditions for mechanical stability are satisfied as[14]:

, ,

,

, , .

From Table S5, it can be concluded that X3NP (X= Ca, Mg) under different pressure satisfy the mechanical stability.

For orthotropic phase X3NP (X = Ca, Mg) (SG Pnma), the Voigt approximate bulk modulus (BV) and shear modulus (Gv), and the Reuss approximate bulk modulus (BR) and shear modulus (GR), are defined as follows[15, 16]:

Among them, Sij are elastic compliance constants. The elastic modulus of Reuss and Voigt are the maximum and minimum values, respectively. Hill believed that the calculation of bulk modulus and shear modulus should take the average of the extreme values[14]. Therefore, Hill average shear modulus and bulk modulus are respectively[15, 16].

Young modulus (Y) and Poisson ratio (ν) can be obtained from G and B, as follows:

Table S5 summarizes elastic constants (Cij), Young’s modulus (Y), bulk modulus (B), shear modulus (G), Poisson’s ratio (υ), and Pugh’s ratio (B/G) for X3NP (X = Ca, Mg) with Pnma (3D) SG under different pressure.

Table S5. The elastic constants (Cij), Young’s modulus (Y), bulk modulus (B), shear modulus (G), and Poisson’s ratio (υ) for X3NP (X = Ca, Mg) with Pnma (3D) SG under different pressure.

| Compounds | Pressure (GPa) | Cij (GPa) |  |  |  |  |  |  |  |  | BVRH (GPa) | GVRH (GPa) | Y (GPa) | υ | B/G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | C11 | C12 | C13 | C22 | C23 | C33 | C44 | C55 | C66 |  |  |  |  |  |
| Ca3NP | 0GPa | 103.3 | 32.2 | 42.3 | 128.7 | 39.7 | 113.2 | 45.5 | 44.6 | 49.4 | 63.5 | 42.8 | 104.9 | 0.2 | 1.5 |
|  | 5GPa | 119.6 | 39.5 | 55.6 | 152.1 | 50.4 | 125.5 | 48.9 | 51.3 | 52.8 | 76.2 | 46.6 | 116.2 | 0.2 | 1.6 |
|  | 10GPa | 138.7 | 46.6 | 68.9 | 176.3 | 63.1 | 140.8 | 52.5 | 58.8 | 55.1 | 90.1 | 50.7 | 128.1 | 0.3 | 1.8 |
|  | 15GPa | 156.6 | 54.3 | 80.7 | 195.6 | 76.4 | 152.6 | 54.7 | 63.3 | 56.4 | 102.8 | 53.2 | 136.0 | 0.3 | 1.9 |
|  | 20GPa | 174.8 | 61.8 | 92.4 | 213.9 | 91.0 | 163.5 | 56.2 | 66.1 | 56.8 | 115.6 | 54.7 | 141.7 | 0.3 | 2.1 |
| Mg3NP | 0GPa | 176.1 | 51.4 | 36.6 | 175.4 | 57.6 | 188.7 | 81.4 | 58.5 | 79.7 | 92.3 | 69.5 | 166.6 | 0.2 | 1.3 |
|  | 5GPa | 200.9 | 57.4 | 43.3 | 196.6 | 71.0 | 201.5 | 88.3 | 63.2 | 84.4 | 104.6 | 74.9 | 181.3 | 0.2 | 1.4 |
|  | 10GPa | 229.2 | 65.8 | 50.9 | 216.5 | 89.0 | 214.9 | 96.0 | 64.2 | 89.1 | 119.0 | 78.9 | 193.8 | 0.2 | 1.5 |
|  | 15GPa | 255.5 | 75.4 | 57.7 | 231.5 | 108.2 | 226.3 | 103.1 | 60.8 | 93.3 | 132.7 | 80.6 | 201.1 | 0.2 | 1.6 |
|  | 20GPa | 280.0 | 85.6 | 64.0 | 243.2 | 127.8 | 236.4 | 109.6 | 54.0 | 97.0 | 145.8 | 80.3 | 203.5 | 0.3 | 1.8 |

Table S6. The ionic (ɛion) and electronic (ɛꝏ) contributions to the static dielectric constant (ɛst) for X3NP (X = Ca, Mg) with Pnma (3D) SG under different pressure.

| Compounds | Pressure | ɛionxx | ɛionyy | ɛionzz | ɛꝏxx | ɛꝏyy | ɛꝏzz | ɛstxx | ɛstyy | ɛstzz |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ca3NP | 0GPa | 16.1 | 16.4 | 14.9 | 7.7 | 7.5 | 7.4 | 23.8 | 24.0 | 22.3 |
|  | 5GPa | 13.6 | 13.2 | 12.1 | 7.6 | 7.5 | 7.4 | 21.3 | 20.7 | 19.5 |
|  | 10GPa | 12.7 | 11.7 | 11.2 | 7.7 | 7.6 | 7.5 | 20.3 | 19.3 | 18.7 |
|  | 15GPa | 12.0 | 10.9 | 10.6 | 7.7 | 7.7 | 7.6 | 19.7 | 18.5 | 18.2 |
|  | 20GPa | 11.4 | 10.3 | 10.3 | 7.8 | 7.8 | 7.7 | 19.2 | 18.1 | 18.0 |
| Mg3NP | 0GPa | 21.0 | 18.9 | 15.0 | 8.8 | 8.9 | 8.6 | 29.7 | 27.7 | 23.6 |
|  | 5GPa | 18.6 | 16.0 | 13.5 | 8.6 | 8.7 | 8.5 | 27.2 | 24.7 | 22.0 |
|  | 10GPa | 16.4 | 13.6 | 12.2 | 8.5 | 8.6 | 8.4 | 24.9 | 22.2 | 20.6 |
|  | 15GPa | 14.6 | 12.0 | 11.3 | 8.4 | 8.6 | 8.4 | 23.0 | 20.6 | 19.7 |
|  | 20GPa | 13.3 | 10.9 | 10.6 | 8.4 | 8.5 | 8.3 | 21.7 | 19.5 | 19.0 |

References

[1] Kresse G, Furthmüller J. Efficiency of ab-initio total energy calculations for metals and semiconductors using a plane-wave basis set. Comp Mater Sci, 1996, 6(1): 15.

[2] Kresse G, Joubert D. From ultrasoft pseudopotentials to the projector augmented-wave method. Phys Rev B, 1999, 59(3): 1758.

[3] Blochl P E, Forst C J, Schimpl J. Projector augmented-wave method: ab initio molecular dynamics with full wave functions. B Mater Sci, 2003, 26(1): 33.

[4] Perdew J P, Burke K, Ernzerhof M. Generalized Gradient Approximation Made Simple. Phys Rev Lett, 1996, 77(18): 3865.

[5] Heyd J, Peralta J E, Scuseria G E, et al. Energy band gaps and lattice parameters evaluated with the Heyd-Scuseria-Ernzerhof screened hybrid functional. J Chem Phys, 2005,123(17): 174101.

[6] Togo A, Tanaka I. First principles phonon calculations in materials science. Scripta Mater, 2015, 108: 1.

[7] Wang V, Xu N, Liu J, et al. VASPKIT: a user-friendly interface facilitating high-throughput computing and analysis using VASP code. Comput Phys Commun, 2021, 267: 108033.

[8] Refson K, Tulip P R, Clark S J. Variational density-functional perturbation theory for dielectrics and lattice dynamics. Phys Rev B, 2006, 73(15): 155114.

[9] Yalameha S, Nourbakhsh Z, Vashaee D. ElATools: A tool for analyzing anisotropic elastic properties of the 2D and 3D materials. Comput Phys Commun, 2022, 271: 108195.

[10] Yu L, Zunger A. Identification of potential photovoltaic absorbers based on first-principles spectroscopic screening of materials. Phys Rev Lett, 2012, 108(6): 068701.

[11] Logan W, Michael W. SL3ME, V1; GitHub repository: https://github.com/ldwillia/SL3ME, 2018.

[12] Chern M Y, Vennos D A, Disalvo F. Synthesis, structure, and properties of anti-perovskite nitrides Ca3MN, M =P, As, Sb, Bi, Ge, Sn, and Pb. J Solid State Chem, 1992, 96(2): 415.

[13] Mochizuki Y, Sung H, Takahashi A, et al. Theoretical exploration of mixed-anion anti-perovskite semiconductors M3XN (M=Mg, Ca, Sr, Ba; X=P, As, Sb, Bi). Phys Rev Mater, 2020, 4(4): 044601.

[14] Hill R. The elastic behavior of crystalline aggregate. Proc Phys Soc A, 1952, 65(5): 349.

[15] Mouhat F, Coudert F X. Necessary and sufficient elastic stability conditions in various crystal systems. Phys Rev B, 2014, 90(22): 224104.

[16] Ravindran P, Fast L, Korzhavyi P A, et al. Density functional theory for calculation of elastic properties of orthorhombic crystals: Application to TiSi2. J Appl Physics, 1998, 84(9): 4891.